## Slide 1: Aircraft Tires
Airframe 02

## Slide 2: Aircraft Tires and Tubes
Aircraft tires may be tube-type or tubeless
Support the weight of the aircraft and provide for traction and braking
Accept static and dynamic stresses in a wide range of conditions

## Slide 3: Tire Classification
Classified by type, ply rating and dimensions
Classified by the United States Tire and Rim association
Type I S.C.
Smooth profile used on fixed gear aircraft designated by their overall diameter.
Found on older aircraft (B-17)
Type III G.A.
Light aircraft with landing speeds less than 160 MPH
Low pressure
Designated by width and diameter of rim tire is mounted on

## Slide 4: Tire Classifications
Type VIII
High performance found on jet aircraft
Known as three part nomenclature tires
High pressure and high load capabilities
Two number system with an X between the numbers (26 x 6.6)
First number is the outside diameter and the second is the width

## Slide 5: Tire Classifications
Type VIII
Three part nomenclature tires
Very high pressure with very high loads
Most modern design of all tires
Combination of type III and type VII numbering systems
Bias tire can be numbered as 30 X 8.8 – 15
Radials use an “R” 30 X 88.8R – 15
Special designators may also include “B” and “H”
“B” - Width ratio is 60-70 percent with a 15 degree bead taper
“H” – Width ratio is 60-70 percent with a 5 degree bead taper

## Slide 6: Ply Rating
Reinforced layers of fabric encased in rubber that are laid into the tire to provide strength
Higher ply ratings are a tire with high strength

## Slide 7: Tube-Type or Tubeless
Designated on sidewall of tire if tubeless
Tubeless tires have inner liner
Consult aircraft manufacturer’s manual for information on tire type needed

## Slide 8: Bias Ply or Radial
Tire can be classified by the direction of plies used in the tire
Traditional tires are bias ply
The angle of the plies in relation to the direction of rotation is 30-60 degrees
Results in flexibility in the side wall
Tire construction
Constructed for usage
Short high impact rather than sustained operations
Deflection is twice as much as automotive tires

## Slide 9: Characteristics of a Tire

## Slide 10: Bead
Important part of an aircraft tire
Anchors the tire carcass and provides a mounting surface for the wheel
High strength carbon steel wire bundles
One , two, or three bead bundles
Bead toe is closest to the wheel
Bead heel transfers the load to the wheel
Chafers protect this area during installation

## Slide 11: Carcass Plies
Casing plies that make up the form of the tire
Each ply consists of fabric sandwiched between two layers of rubber
Angle is manipulated to create a bias or radial
Radials require fewer plies than bias
Protective layers are made up of nylon reduce distortion and increase stability
Protective plies also resist puncture and cutting

## Slide 12: Tread
Tread is the crown area made to contact the ground
Rubber compound formulated to resist wear, abrasion, cutting, and cracking
Most tires have circumferential grooves
Older aircraft that have differential steering may not have grooves
Designed to stabilize aircraft on operating surfaces
Some tires are designed to recapped
Consult manufacturer’s data for guidance

## Slide 13: Sidewall
Layer of rubber designed to protect carcass plies
May contain ozone resistant qualities
Information about the tire is located here
Tube tire has thin inner liner
Tubeless tire have a thicker liner for less permeability
Small amounts of air seep out through sidewall vents
Green or white dot that must be kept clear
Trapped gas could cause ply separation
Tube tire also have vent for the air between the tube and the tire

## Slide 14: Chine
Some tires have sidewalls that form a chine
A built in deflector
Deflects water away from fuselage mounted engines

## Slide 15: Tire Inspection
Inspection occurs on a regular basis
Sidewall, inflation, and tread wear
Inflation
Aircraft manufacturer’s data must be consulted for inflation pressures
Do not inflate by pressure on the side of tire or by looks
Check pressure while under load
Can vary as much as 4 percent
Calibrated gauge should always be used to measure pressure

## Slide 16: Tire Inspection
Tire disperse energy and heat
Structural damage can occur in extreme heating situations
Improper inflation
Can cause internal damage
May flex beyond it’s designed capabilities
Check daily or before flight
Measure at ambient temperature
Pressure changes 1 percent for every five degrees
Flown from one place to another may change pressures
Allow 3 hours after landing to check
May creep or slip if underinflated
Dual wheel assemblies require both tire to be replaced when damage occurs to one due top uninflation

## Slide 17: Tire Inspection

## Slide 18: Tread Condition
Condition of trend must be ascertained with tire inflated and installed on aircraft
Tread depth and wear patterns
Evenly worn tread is a sign of proper tire maintenance
Uneven wear should be examined
Remove any tire that guidance is unavailable for if wear is down to bottom of groove for more than 1/8 inch of the circumference
A properly maintained tire reaches its wear limits along the center of the tire

## Slide 19: Tread Condition
Asymmetrical tread wear may be caused by misalignment
Sometimes may be due to landing gear geometry
May be caused by taxiing on a single engine or tight high speed turning
Tire may be removed and turned around to balance wear
Removing tire prior to wear limits makes it eligible for tire retreading
Consult manufacturer’s specifications for limits

## Slide 20: Tread Damage
In addition to wear tires must be inspected for damage
Cuts, bruises, bulges, imbedded foreign objects, chipping
Mark damaged areas before tire removal
Remove embedded objects only if not beyond the tread otherwise deflate
Examine hole to determine damage
If 3/8 or less it is acceptable
Exposed casing cord body is unairworthy

## Slide 21: Tread Damage
Cuts across tread rib are cause for removal
Can lead to rib peel
Flat spots are a result of tire skidding
If ply is exposed tire must be removed
If balance is affected remove tire
Bulge or separation is cause for removal
Grooved runways can cause several chevron shaped cuts
Ok for continued use unless chunking or cuts result
Chunking should not expose more than 1 inch

## Slide 22: Tread Damage

## Slide 23: Tread Damage
Cracking in tread groove is usually not acceptable if ¼ inch or more of tread is exposed
Groove cuts usually cause the entire tire tread to be thrown

## Slide 24: Tread Damage
Fluids can soften tires and make them spongy
A contaminated tire must be removed from service
Wash with Denatured alcohol and soap and water
Protect tires from potential contact

## Slide 25: Sidewall Damage
Primary purpose is to protect the carcass
Cuts, abrasions, gouges, snags, and other injuries the tire must be replaced
Mark the area
Circumferential cuts are not acceptable
Bulges indicate separation and tire must be replaced
Cracking and checking to cords tire must be replaced
Checking that does not affect performance may be acceptable

## Slide 26: Tire Removal
Consult aircraft manufacturer instructions for procedures
Ensure proper safety precautions are taken
Tire can be under high pressure
Damage tires risk explosion
Approach damaged tire from oblique angle
Deflate tires before removal
Use valve core tool
Stand to the side

## Slide 27: Tire Removal
Separate tire from wheel assembly
Must break bead
Use proper equipment
Break bead with wheel tie bolts installed and tight
Use tool to break bead placing it as close to the wheel as possible
Apply pressure slowly to avoid damage to sidewall
Soapy solution may be used to help process

## Slide 29: Inspection off the Aircraft
43-13-1 gives guidelines for tire inspection and repair
Closely examine bead area
Damage is cause for rejection
Thermal plug melting require tire replacement
Duals require both tire to be replaced
Cuts cannot exceed 40 percent of the tire
Punctures 1/8 inch and less can be repaired
Exposed cords on sidewall are cause for rejection

## Slide 30: Tire Repair and Retreading
Follow airframe and tire manufacturer’s recommendations
All tire repairs must be made at a certified tire repair facility
Technician must determine if tire is eligible for retreading
FAA certified tire repair station will make the ultimate decision
Shearology will be conducted to ensure carcass is in serviceable condition
Tires are marked if retreaded
Can be retreaded a number of times
Nose tires sometimes make it to 12 retreads

## Slide 31: Tire Storage
Can be damaged if not stored properly
Stored vertically resting on tread surface
Storing on rack with 3-4 inch flat surface is recommended
Only stack horizontally for a short period of time
No higher than 4 tires if under 40 inches
No higher than 3 for tires larger than 40 inches
Store in cool, dry, dark place free from air currents and dirt
O2 and O3 can cause deterioration of tires
O3 producing equipment can harm tires
Fuels, oils, solvents do harm
Moisture and dirt prone areas should be avoided
Store in temperatures between 32-104 F
Lower temps are acceptable, but not higher

## Slide 32: Aircraft Tubes
Tube construction and selection
Tubes are made of natural rubber
Contain air with minimal leakage
Heavy duty tubes are available
Fabric is incorporated to protect against heat from braking
Tubes come in a variety of sizes
Too small of a tube stresses tube construction
Storage and Inspection
Keep in carton until installation
Wrap in paper if carton is unavailable
Can be stored in tire inflated enough to hold shape for a minimum time
Apply talc to avoid sticking
Avoid creases when storing
Never hang on nails or pegs for storage